Scintillating Fibers – analysis report
Kasia Rusiecka
May 2018

---
January measurements – setup and collected data
SiPM model: S13360-3050VE
Evaluation board: C12332-01
Power supply: C11204-01
Series number	Fiber type	Number of measurements	Source	Source positions [mm]	Description
1	LuAG:Ce (1) Crytur	9	Na-22 6MBq	10.3, 20, 30, 40, 50, 60, 70, 80, 90	First measurement
2	LuAG:Ce (2) Crytur	9	Na-22 6MBq	10.2, 20, 30, 40, 50, 60, 70, 80, 90	First measurement
3	LuAG:Ce (1) Crytur	9	Na-22 6MBq	10.4, 20, 30, 40, 50, 60, 70, 80, 90	Remeasured
4	LuAG:Ce (2) Crytur	9	Na-22 6MBq	10.5, 20, 30, 40, 50, 60, 70, 80, 90	Remeasured
5	LuAG:Ce (1) Crytur	9	Na-22 6MBq	10.4, 20, 30, 40, 50, 60, 70, 80, 90	With Al coating
6	LuAG:Ce (1) Crytur	5	Na-22 6MBq	50, 50, 50, 50, 50	Influence of different couplings
7	LuAG:Ce (1) Crytur	1	-	-	Internal activity measurement
8	LuAG:Ce (2) Crytur	1	-	-	Internal activity measurement
9	-	2	-	-	PE calibration
 1

---
ScintillatingFibers – software structure
Preparatory classes
Analysis classes
SFData
Loads and prepares experimental data. Returns: spectra of all types (single/series), signals (single/averaged), ratio histograms (single/series). Custom cuts on data possible.
SFAttenuation
Determines attenuation length using two methods: (1) using averaged signal from two ends of fiber, (2) separately for each fiber end. Returns numerical values as well as attenuation graphs.
SFMC
Loads data from Monte Carlo simulations. Returns spectra of requested type and with custom cut. Necessary for the template fit.
SFTimingRes
Determines timing resolution using two methods: (1) excluding scattered events only, (2) with the cut on 511 keV peak and excluding scattered events. Returns numerical values, timing spectra and graph ch_0.T0 – ch_1.T0 vs. source position.
BGFit
Functions used for fitting in other classes. Contains: Pol2, Pol3, Expo.
SFTimeConst
Determines time constants of recorded signals: rise time and decay time in two modes – single decay and double decay. Returns signals with fitted functions and numerical values.
SFPeakFinder
Locates 511 and 1270 keV peaks and performs background subtraction. Returns background-subtracted peak, its range and other parameters, e.g. position, sigma.
TFit
Class for the template fit.
On-line class reference [link]
 2

---
Raw data examples - signals
Series 3, channel 1, source position 50 mm,
20 signals of PE ~100 averaged
Series 3, channel 0, source position 50 mm,
20 signals of PE ~100 averaged
Series 3, channel 1, source position 50 mm, first signal with amplitude between 50 and 70 mV
Series 3, channel 0, source position 50 mm, first signal with amplitude larger than 200 mV
 3

---
Raw data examples – charge spectra
Series 3, channel 0,
source position 10 mm
Intrinsic activity + scattered photons
Compton edge
Compton edge
1270 keV photopeak
511 keV photopeak
 4

---
Attenuation length – averaged signal from both channels
M_{FB}(z) = sqrt{{ ch_0 (z) } over { ch_1 (z) }}
ln(M_{FB}(z)) = A_0 + z over L_att
Series 3 – attenuation curve
Series 4 – attenuation curve
Series 5 – attenuation curve
Latt = (284.40 ± 0.37) mm
Latt = (265.72 ± 0.36) mm
Latt = (207.51 ± 0.28) mm
LuAG:Ce Fiber #1
LuAG:Ce Fiber #2
LuAG:Ce Fiber #1 with Al wrapping
 5
ln(MFB)
ln(MFB)
ln(MFB)

---
Attenuation length – independent channels
Series 3 Channel 1
Series 3 Channel 0
LuAG:Ce Fiber #1
Latt ch0 = (306.18 ± 0.88) mm
Latt ch1 = (188.66 ± 0.35) mm
(Latt ch0 + Latt ch1)/2 = 247.42 mm
Series 4 Channel 0
Series 4 Channel 1
LuAG:Ce Fiber #2
Latt ch0 = (188.08 ± 0.35) mm
Latt ch1 = (260.82 ± 0.67) mm
(Latt ch0 + Latt ch1)/2 = 224.45 mm
Series 5 Channel 1
Series 5 Channel 0
LuAG:Ce Fiber #1 with Al coating
Latt ch0 = (234.29 ± 0.53) mm
Latt ch1 = (153.61 ± 0,23) mm
(Latt ch0 + Latt ch1)/2 = 193.95 mm
 6

---
Background subtraction – example
Series 5, channel 1
 7

---
Timing resolution – cut on scattered events
Ch_0.fT0 – Ch_1.fT0, position 10 mm
Ch_0.fT0 – Ch_1.fT0, position 20 mm
Ch_0.fT0 – Ch_1.fT0, position 30 mm
Series 3
LuAG:Ce Fiber #1
Ch_0.fT0 – Ch_1.fT0, position 60 mm
Ch_0.fT0 – Ch_1.fT0, position 50 mm
Ch_0.fT0 – Ch_1.fT0, position 40 mm
Ch_0.fT0 – Ch_1.fT0, position 70 mm
Ch_0.fT0 – Ch_1.fT0, position 80 mm
Ch_0.fT0 – Ch_1.fT0, position 90 mm
 8

---
Timing resolution – cut on scattered events
Ch_0.fT0 – Ch_1.fT0, position 10 mm
Ch_0.fT0 – Ch_1.fT0, position 20 mm
Ch_0.fT0 – Ch_1.fT0, position 30 mm
Series 4
LuAG:Ce Fiber #2
Ch_0.fT0 – Ch_1.fT0, position 60 mm
Ch_0.fT0 – Ch_1.fT0, position 50 mm
Ch_0.fT0 – Ch_1.fT0, position 40 mm
Ch_0.fT0 – Ch_1.fT0, position 70 mm
Ch_0.fT0 – Ch_1.fT0, position 80 mm
Ch_0.fT0 – Ch_1.fT0, position 90 mm
 9

---
Timing resolution – cut on scattered events
Ch_0.fT0 – Ch_1.fT0, position 10 mm
Ch_0.fT0 – Ch_1.fT0, position 20 mm
Ch_0.fT0 – Ch_1.fT0, position 30 mm
Series 5
LuAG:Ce Fiber #1 +
Al coating
Ch_0.fT0 – Ch_1.fT0, position 60 mm
Ch_0.fT0 – Ch_1.fT0, position 50 mm
Ch_0.fT0 – Ch_1.fT0, position 40 mm
Ch_0.fT0 – Ch_1.fT0, position 70 mm
Ch_0.fT0 – Ch_1.fT0, position 80 mm
Ch_0.fT0 – Ch_1.fT0, position 90 mm
10

---
Timing resolution – energy cut on 511 keV peak + scattered events
Ch_0.fT0 – Ch_1.fT0, position 10 mm
Ch_0.fT0 – Ch_1.fT0, position 20 mm
Ch_0.fT0 – Ch_1.fT0, position 30 mm
Series 3
LuAG:Ce Fiber #1
Ch_0.fT0 – Ch_1.fT0, position 60 mm
Ch_0.fT0 – Ch_1.fT0, position 50 mm
Ch_0.fT0 – Ch_1.fT0, position 40 mm
Ch_0.fT0 – Ch_1.fT0, position 70 mm
Ch_0.fT0 – Ch_1.fT0, position 80 mm
Ch_0.fT0 – Ch_1.fT0, position 90 mm
11

---
Timing resolution – energy cut on 511 keV peak + scattered events
Ch_0.fT0 – Ch_1.fT0, position 10 mm
Ch_0.fT0 – Ch_1.fT0, position 20 mm
Ch_0.fT0 – Ch_1.fT0, position 30 mm
Series 4
LuAG:Ce Fiber #2
Ch_0.fT0 – Ch_1.fT0, position 60 mm
Ch_0.fT0 – Ch_1.fT0, position 50 mm
Ch_0.fT0 – Ch_1.fT0, position 40 mm
Ch_0.fT0 – Ch_1.fT0, position 70 mm
Ch_0.fT0 – Ch_1.fT0, position 80 mm
Ch_0.fT0 – Ch_1.fT0, position 90 mm
12

---
Timing resolution – energy cut on 511 keV peak + scattered events
Ch_0.fT0 – Ch_1.fT0, position 10 mm
Ch_0.fT0 – Ch_1.fT0, position 20 mm
Ch_0.fT0 – Ch_1.fT0, position 30 mm
Series 5
LuAG:Ce Fiber #1
+ Al coating
Ch_0.fT0 – Ch_1.fT0, position 60 mm
Ch_0.fT0 – Ch_1.fT0, position 50 mm
Ch_0.fT0 – Ch_1.fT0, position 40 mm
Ch_0.fT0 – Ch_1.fT0, position 70 mm
Ch_0.fT0 – Ch_1.fT0, position 80 mm
Ch_0.fT0 – Ch_1.fT0, position 90 mm
13

---
title
00